## Slide 1: Results and Plans of the SOIPIX Collaboration
K. Hara (University of Tsukuba)
SOIPIX Collaboration:
KEK, U. Tsukuba, Osaka U., Tohoku U., Kyoto U., Kyoto U. of Education,
JAXA/ISAS, RIKEN, LBNL, FNAL, U. Hawaii, INP Krakow, INFN Padova, OKI Semiconductor Co. ,Ltd.
corporation with Tohoku-Micro Tech Co. ,Ltd.
Collaboration was formed in 2005 by KEK-Universities (Y. Arai, representative) to develop monolithic pixel devices utilizing Silicon-On-Insulator technology provided by OKI Semiconductor

## Slide 2: Monolithic SOI Pixel Device
Technology characteristics:
bonded SOI wafers by SOITEC Co. with high resistive (~700Wcm) “handle wafer” for sensing part
commercial FD-SOI process (0.20mm) by OKI Semiconductor
Pros:
monolithic
(fab. cost, small material, high density,,,)
SOI features
(low power, hi-speed, no latch-up,
4K-300C operational,,,)
Cons:
back-gate effect
(readout affected by the bias voltage)
BPW, 3D
MPW runs this year: 5 metal layers, MIM(1.5 fF/mm2)
200nmBOX
40nmSi
Main process parameters:

## Slide 3: Multi-project wafer
MPW:
to boost SOI device developments
3D process possible (3D_L, 3D_U)
20.8mm sq on 8” wafer
FY09-2
FY09-1

## Slide 4: Coming MPW – layout plan -
We schedule twice in this FY (~Mar.2011) :
Aug.2010 & Jan.2011 submissions
We call your participation. Please visit:
http://rd.kek.jp/project/soi/MPWrun
FY09-1

## Slide 5
1. Integration-Type Pixel detector (INTPIX)
2. Counting-Type Pixel detector(CNTPIX)
FY09-1
INTPIX3b
INTPIX4
CNTPIX4
2005 2006 2007 2008 2009 2010
FY05
MPW
(VDEC)
PIXELTEG
(INTPIX)
SOI pixel detector development –Overview-
FY06
MPW
0.15um
Process
INTPIX1
CNTPIX1
FY07
MPW
0.2um
Process
INTPIX2
CNTPIX2
FY08
INTPIX3
CNTPIX3
Two main types of pixel detectors designed by KEK:
FY09-2
INTPIX3c
CNTPIX5

## Slide 6: SEABAS DAQ system
Ethernet
ROOT GUI software
SEABAS=Soipix EvAluation BoArd with SiTCP*
-packaged chip is mounted on sub-board
-65MHz 12-bit ADC (for INTPIX)
- 4 ch 12bit DAC
-User FPGA controls
-SiTCP(network processor) for TCP/IP
-light weight DAQ system (portable)
sub-board
Packaged
chip
* T. Uchida and M. Tanaka, “Development of a TCP/IP Processing Hardware”, IEEE Nuclear Science Symposium, San Diego, USA, Oct. 29 - Nov. 4, 2006, NSSproc. N33-6, 1411 – 1414.
All the data acquisition are done with the SEABAS

## Slide 7: Integration type pixel (INTPIX)
INTPIX3 (128x128 pixels)
pixel (20x20mm) with 4 p+ contacts
APS type readout on each pixel
20mm
Block diagram
Mask image for red laser

## Slide 8: Counting type pixel (CNTPIX)
Signals within energy window (dual thresholds) are counted per pixel via a 16-bit counter (designed after Medipix2)
CNTPIX2.1 (128x128)
Brass mask image to 8 keV X-ray
Tint=16ms
Vback=20V
p-n junctions
Analog
16b
Counter
9b Register
DDL
64um
~600 transistors/pixel

## Slide 9: R&D issues
Larger area (with SEABASII)
Process optimization
  Optimization of BPW, including nested BWs
  Cross-talk suppression
  Higher bias application (electrode shape optimization)
  FZ wafers (P-bulk) SOI
  Wafer thinning (full depletion, backside illumination)
  Lower noise (CDS)
Radiation tolerance
3D integration
CDS: Correlated double sampling

## Slide 10
larger pixel:
INTPIX4
Single BPW
17mm
-Pixel size reduced to 17mm
-2 types of pixels:
Single BPW or floating BPW ring
Pixel circuit (CDS)
New readout system board (SEABAS2:Gigabit & multiple ADCs) will be used
Overall: 10.2x15.4mm
- # of pixels: 512 x 832 pixels
- 13 Analog Out (13x512x64)

## Slide 11
Counting Type Pixel (CNTPIX5)
D
D
CNTPIX5
218 x 72 pixels
1pixel (64x64mm)
14.0x4.6mm
active area
pixel size: 64x64 um2
BPW in a pixel
Counter option: 9bit x 2 or 18bit
Preamplifier + Shaper
Binning mode: 2x2 pixels  9b x 8 store
Shape good for tiling
(with SEABAS2)

## Slide 12
CNTPIX4 response - Red laser (635nm)
Metal mask
- Circuit works successfully
- No major problem in the circuit
Evaluating noise level, pulse laser response (ongoing)
Evaluation of INTPIX5 is ongoing
COL(0-71)
ROW(0-215)
100
0
Notes: 12

## Slide 13
BPW Implantation
Suppress the back gate effect.
Increase break down voltage with lower dose BPW-n junction.
Less electric field in the BOX which should enhance e-h recombination, thus may improve radiation hardness.
BPW
P+
SOI Si
Buried
Oxide
(BOX)
Cut top Si and BOX, high dose
Low dose not to affect top Si
Substrate Implantation
Pixel
Peripheral
Buried p-Well (BPW) Process
n
BNW reduces the pixel-electronics coupling
BNW could be used to compensate the radiation induced threshold shifts
(start with positive BNW, lower the voltage as positive charge is accumulated in BOX)
BNW, BPW nested
(available in coming MPWs)

## Slide 14: BPW effectiveness
Transistor characteristics is not affected by the backgate voltage up to 100V for BPW=0V.
Similar results for PMOS
w/ BPW=0V
w/ BPW=Floating
Vgs [V]
Vgs [V]
DVth < 3mV
Vgs [V]
NMOS transistor Id-Vg curves evaluated with TrTEG
w/o BPW
Vs=0 V
Vd=1.8V

## Slide 15
window
focused inside
Pulsed 1064 nm YAG:Nd laser (base width~10ns)
INTPIX3 (w. BPW) response to 1064nm laser
- Signal increases up to 130 V (just below breakdown )
Back-gate effect is suppressed
BPW only under the peripheral circuit R4 reduces the effect…
 penetration depth ~3mm
K. Hara - VERTEX2010, 6-11 June, Loch Lomond, Scotland

## Slide 16: Cross-talk: BPW design for pixels
While injecting laser to one pixel,
adding neighbors (3x3) increases notably in region 5
adding further neighbors (5x5) stays similar
region 1
region 5
p+
p+
separate BPW electrodes
large BPW electrode tied to the readout p-implants

## Slide 17
  Higher bias application
Better with sq->oct and/or wo->w BPW
Circle is available in coming MPWs
<IR camera>
corner of NS ring is weakest

## Slide 18: Wafer thinning by DISCO-TAIKO
OKI-semi process on 725mm thick 8” wafer
Usual chips: thinned to 260mm and Al sputtered on back
One wafer (incl. INTPIX2) thinned to 106 mm by DISCO Co.
process: TAIKOTM grinding + chemical etching
  No backside aluminization tried
  Full depletion expected at 60 V
From DISCO web:
Grind leaving an edge ~3mm
50um thickness possible for 8”
negligible grind-originate warp
zero edge chipping
self sustainable
easier handling
post process possible
Photo: http://www.disco.co.jp/jp/solution/library/taiko.html
TAIKO=drum

## Slide 19: Thinned wafer and chips
Typical profile (0.4 mm max for 40x80 mm block)
Warp introduced by residual strain caused by
CTE difference between Si and SiO2
IV of 5 INTPIX2 chips (A-E) compared
before(690um) and after(105um)
Small change in leakage current plateau
Small change in breakdown onset voltage

## Slide 20: Thinned INTPIX2 response
INTPIX2(105um)
INTPIX2(260um)
INTPIX3(260um)
0 10 20 30 40 50 60 70
Vback[V]
Thinned INTPIX2 responded properly
This is our first successfully thinned chip
INTPIX2(105um)
INTPIX2(260um)
Pedestal shifts
Larger shift due to back-gate effect, although substantial in INTPIX2 of normal thickness.
Response to white light
(pedestal adjusted)
Quicker decrease in thin INTPIX2
- Flat response expected if no back-gate effect
Thinning INTPIX3 wafer is in progress, where we expect to observe full depletion

## Slide 21: Radiation Effects to NMOS (Co irradiation)
(top plots) Tr I-V is distorted as Vback is raised, if no BPW
(bottom) Tr I-V is unchanged up to Vback=100V, if BPW=0V
w/o BPW
w/ BPW
=0V
Vgs [V]
Vgs [V]
Vgs [V]
Vgs [V]
0.20 kGy
2.0 kGy
Vgs [V]
22 kGy
5.0 kGy
start to deviate
distortion
preliminary

## Slide 22: Vth shifts by 70-MeV protons and 60Co
Chart: Dose [ 1-MeV neq/cm2]
| 100000000000 | 1350000000000 | 12800000000000 | 602000000000000 | 1180000000000000
Tr=3 | 0 | -0.02904 | -0.13142 | -0.6197 | -0.77984
Tr=4 | 0 | -0.058253 | -0.15536 | -0.60582 | -0.74109
Tr=6 | 0 | -0.049633 | -0.084196 | -0.40295 | -0.56922
60Co g
pre-irrad
shifts by protons and Co are similar : rebound in NMOS
Main reason for the threshold shifts is charge states trapped in oxide, mainly in BOX (estimated from TCAD simulation).
The thresholds shifts are recoverable by annealing (confirmed for samples irradiated to 2 kGy X-ray)
70-MeV protons
Tr3-5: tOX=7.0nm
Tr6: tOX=4.5nm

## Slide 23: 3D: T-Micro
Tohoku-Micro Tec Co.
VIA first
Koyanagi group has technologies for 3D
Via, ConC/ConW self alignment, m-bond, adhesive injection

## Slide 24: 3D: m-Bond Process Flow for SOIPIX

## Slide 25: Wafer Bonding by m-Bumps
SEM for test SOI chips
Metal bumps (In/Au) are created by lift-off method
Good mechanical bonding is provided by adhesive

## Slide 26: Bonded SOI

## Slide 27: Schematic of m-bump

## Slide 28: m-Bumps

## Slide 29: Summary
SOI monolithic pixel devices, INTPIX and CNTPIX mainly, are developed successfully showing ingenious feature in detecting visible/IR light and X-rays.
Buried p-Well is a technological breakthrough in suppressing the back-gate effect.
Further R&D is on-going including
  Thinning by TAIKO process
  Larger INTPIX and CNTPIX detectors
  Charged particle detection
  Radiation effect study
Vertical (3D) integration is one of the key technologies for further SOI pixel detector developments.
We are operating SOI MPW run twice per year. We welcome more and more participants to make the technology further established.

## Slide 30: Adhesive injection

## Slide 31: BPW designs for on-pixel electronics
1
2
3
4
5
6
7
8
Regions 1-3,7 ：1p readout
No BPW in R4 and R8 (under transistors)
Region 2
Region 5
Region 4
(no BPW)
Region 8
BPW=yellowish
p+
p+